SEMQuant results. Listed at 14:04:26 PM on 20/06/2013

Operator: Do SEM 24hr.

Client: Do SEM 24hrs.

Job: Do SEM Services.

Spectrum label: brake350

System resolution =  62 eV

Quantitative method: ZAF ( 4 iterations).

Analysed elements combined with: O ( Valency: -2)

Method : Stoichiometry Normalised results.

Nos. of ions calculation based on  1 cations per formula.

Standards :

C  K      CaCO3 01/12/93

Mg K      MgO 01/12/93

Al K      Al2O3 23/11/93

Si K      Quartz 01/12/93

P  K      GaP 29/11/93

S  K      FeS2 01/12/93

K  K      MAD-10 02/12/93

Ca K      Wollas 23/11/93

Ti K      Ti 01/12/93

Mn K      Mn 01/12/93

Fe K      Fe 01/12/93

Cu K      Cu 01/12/93

Ba L      BaF2 01/12/93

Elmt   Spect. Element  Atomic           Compound   Nos. of

Type     %       %                 %        ions

C  K     ED    10.32    18.21   CO2       37.80      0.52

Mg K     ED     0.34     0.30   MgO        0.57      0.01

Al K     ED     1.15     0.91   Al2O3      2.18      0.03

Si K     ED     2.61     1.97   SiO2       5.58      0.06

P  K     ED     0.21     0.14   P2O5       0.48      0.00

S  K     ED     2.66     1.76   SO3        6.64      0.05

K  K     ED     2.26     1.22   K2O        2.72      0.03

Ca K     ED     1.22     0.64   CaO        1.70      0.02

Ti K     ED     8.06     3.57   TiO2      13.44      0.10

Mn K     ED     0.08*    0.03*  MnO        0.10*     0.00*

Fe K     ED    10.94     4.15   Fe2O3     15.63      0.12

Cu K     ED     3.64     1.21   CuO        4.56      0.03

Ba L     ED     7.71     1.19   BaO        8.61      0.03

O              48.82    64.70                        1.83

Total         100.00   100.00            100.00

Anion sum   1.83

* = <2 Sigma